Mesh Membrane

An Ultra Low Disturbance

Building Solution for walls

Introduction

Mesh Membrane is a plastic, dimpled sheet material with a polypropylene mesh welded to one surface.

It can used to provide a new interior surface inside buildings for direct plastering, where the walls are old, salt contaminated or damp.

DESCRIPTION

Trade Mesh Membrane is a plastic, dimpled sheet supplied on a 2 metre wide roll,

10 metres in length.

The surface has a welded polypropylene mesh for direct plastering with normal lightweight plasters.

TECHNICAL DATA

Material

Studded Polyethylene, 7mm thick

Other Components

Plastic plugs, mastic rope, tape for joints

Size

Roll 2.05 metres wide with overlaps, 10 metres long giving an effective area of cover of 20 square metres

Fixing size

White large headed plugs are 10mm diameter x 70mm long

Hole size for drilling

Drill 8mm diameter holes, 80mm deep

Fixing spacing

At 250mm centres = 25 per square metre

PROPERTY REPAIR SYSTEMS

Tel: 01626 331351  Fax: 01626 331143

Special features

·	Easy fix hammer in plugs

·	Plaster directly on mesh

·	Mastic rope included

·	Provides new, dry surface

·	Joint tape for overlaps

·	Guaranteed

2m x 10m TRADE KIT

BBA Cert. No:05/4261

USES

To provide new, dry surfaces in old buildings where the walls have been contaminated with ‘salts’ or dampness, but only where no liquid water is present. (Can also be used as part of full cellar or basement conversions, with non-mesh membrane flooring and the addition of a sump pump.)

PREPARATION & APPLICATION

Hack off all plaster and contaminated render to bare brick or stone. Brush off all loose material. Check the roll size compared to the wall areas to be covered, allowing for an overlap between sheets of 100mm. Keep all materials dust free during cutting and fixing.

Prepare the plugs by fitting a small length of mastic rope around the underside of each plug head, to seal against water vapour ingress. Drill 8mm holes about 80mm deep. Hammer the fixing plugs through the membrane until the seals are squeezed against the sheet surface. When butting sheets together apply the black, butyl tape to the three hole overlap (no mesh) and press surfaces firmly together. Allow an air gap top and bottom, to ventilate the air space.

Plaster with Carlite Bonding, Tilcon Whitewall, 1:1:6 lime sand render or fix plaster board with adhesive dabs.