Slimline Floorseal

An Ultra Low Disturbance

Building Solution for damp floors

Introduction

Slimline Floorseal Membrane is a plastic, dimpled sheet material for floor applications.

It can be used to provide new interior floor surfaces inside buildings, where the floors are old, salt contaminated or damp. New concrete can be immediately covered for installation of timber flooring.

DESCRIPTION

Slimline Floorseal Membrane is a plastic, dimpled sheet supplied on a 2 metre wide roll 20 metres in length. The surface can be directly fitted with a ‘floating’ floor (chipboard, 22mm) or screeded (minimum of 2 inches, 50mm thick).

TECHNICAL DATA

Material

Studded Polyethylene, 2mm thick, made from 0.5mm, 2500 gauge plastic

Other Components

Tape for joints, corner tape

Size

Roll 2.08 metres wide, 20 metres long giving an effective area of cover of 36 square metres (after deducting overlaps)

Compressive Strength

180 k/N per square metre

PROPERTY REPAIR SYSTEMS

Tel: 01626 331351 Fax: 01626 331143

Special features

·	Easy lay on the floor, no fixings, with taped joints

·	Only 2mm thick

·	Guaranteed instant dry floor

Only 2mm thick

Concrete floor covering

USES

To provide new, dry surfaces in old buildings where floors have been contaminated with ‘salts’ or dampness, or are partially below ground level, (but only where no liquid water is present – otherwise use Kontract Membrane, to allow enough stud height for drainage).

It can also be used for new concrete, as a fast track way of laying timber flooring or tiling, without waiting for the concrete to fully dry.

PREPARATION & APPLICATION

Old Floors – use Kontract Membrane and install sub floor drainage, if liquid water is ever present.

Lay Slimline Floorseal Membrane grooved side down. Tape the joints. Use Corner Tape at floor to wall junction. Lay insulation (optional) under treated chipboard or, for uneven floors apply a 50mm sand/cement screed.

New Floors - lay Slimline Floorseal Membrane grooved side down. Tape the joints. Use Corner Tape at floor to wall junction. Lay insulation (optional) under treated chipboard or, for uneven floors, apply a 50mm sand/cement modified screed. Use Bondacryl to enhance the screed strength, to avoid any risk of cracking.

DCM/01/09